Table-2. Characterization of PCL scaffold. Data are presented as mean±SD.

|  |  |  |  |
| --- | --- | --- | --- |
| **Fiber diameter (nm)** | **Tensile strength (MPa)** | **Porosity (%)** | **Contact angel (0)** |
| 692±72 | 3.01±0.74 | 70.1±5.3 | 76.7±0.9 |