Table-2. Characterization of PCL scaffold. Data are presented as mean±SD.

| Fiber diameter (nm) | Tensile strength (MPa) | Porosity (%) | Contact angel (0) |
| --- | --- | --- | --- |
| 692±72 | 3.01±0.74 | 70.1±5.3 | 76.7±0.9 |