| Table 1. Properties of gelatin films incorporated with Ferula oil (FAO). |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Pure gelatin | Gelatin-FAO 2% | Gelatin-FAO 4% | Gelatin-FAO 6% | Gelatin-FAO 8% |
| Solubility (%) | 29 ± 1.6c | 30 ± 1.3c | 33 ± 1.2b | 34 ± 1.2b | 37 ± 1.6a |
| Swelling (%) | 396 ± 8a | 381 ± 9ab | 368 ± 6bc | 355 ± 9cd | 344 ± 5d |
| WVP (g.mm/m2.h) | 0.23 ± 0.018d | 0.24 ± 0.012c | 0.26 ± 0.014bc | 0.29 ± 0.018ab | 0.32 ± 0.015a |
| Tensile strength (MPa) | 4.2 ± 0.42a | 3.7 ± 0.21ab | 3.2 ± 0.23bc | 2.9 ± 0.22cd | 2.6 ± 0.13d |
| Elastic modulus (MPa) | 5.8 ± 0.42a | 5.2 ± 0.25ab | 5.2 ± 0.25ab | 4.1 ± 0.42cd | 3.6 ± 0.22d |
| Elongation at break (%) | 128 ± 7d | 139 ± 6cd | 145 ± 8bc | 158 ± 5ab | 165 ± 7a |
| Opacity | 15 ±1.5c | 19 ± 2.2bc | 21 ± 2.6ab | 23 ± 2.8a | 26 ± 3.3a |
| Antioxidant activity (mg AAE / g film) | 0.42 ± 0.05e | 0.70 ± 0.1d | 2.06 ± 0.2c | 2.82 ± 0.4b | 3.86 ± 0.5a |
| Mean values with different letters within a raw are significantly different by Duncan’s multiple range tests at p < 0.05. The antioxidant activity was expressed milligram ascorbic acid equivalent (AAE) per gram incorporating different concentrations of Ferula oil. |  |  |  |  |  |

| Table 2. Antibacterial activity of gelatin film incorporated with Ferula oil (FAO). |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | Inhibition zone diameter (mm) |  |  |  |
| Films | S. aureus | B. Subtilis | E. coli | P. aeroginosa |
| Pure gelatin | 0 ± 0c | 0 ± 0c | 0 ± 0b | 0 ± 0b |
| Gelatin + FAO 2% | 30 ± 1.2b | 30 ± 0.9b | 30 ± 1a | 30 ± 0.7a |
| Gelatin + FAO 4% | 31 ± 1b | 31 ± 0.8ab | 30 ± 1.2a | 30 ± 0.8a |
| gelatin + FAO 6% | 32 ± 1.5ab | 32 ± 1.1a | 31 ± 1.6a | 30 ± 1.3a |
| Gelatin + FAO 8% | 34 ± 1.7a | 33 ± 1.3a | 32 ± 1.7a | 31 ± 1.5a |
| Antibacterial activity was expressed as diameter of bacterial growth inhibition zone in the presence of films with different Ferula oil concentration. Mean values with different letters within a column are significantly different by Duncan’s multiple range tests at p < 0.05. |  |  |  |  |

| Table 3. The antibacterial activity of gelatin film incorporated with Ferula oil (FAO). |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | Colony reduction (%) |  |  |  |
| Films | S. aureus | B. Subtilis | E. coli | P. aeroginosa |
| Pure gelatin | 0 ± 0e | 0 ± 0d | 0 ± 0e | 0 ± 0e |
| Gelatin + FAO 2% | 46.3 ± 2.4d | 62.8 ± 3.6c | 17.4 ± 2d | 1.73 ± 1d |
| Gelatin + FAO 4% | 75.9 ± 3.3c | 83.4 ± 3.3b | 61 ± 4.2c | 31.8 ± 3c |
| gelatin + FAO 6% | 89.6 ± 3.6b | 92.5 ± 4.2a | 83.4 ± 3.2b | 63.6 ± 4.7b |
| Gelatin + FAO 8% | 100 ± 4a | 98.5 ± 3.8a | 96.6 ± 5a | 90.2 ± 4.5a |
| Antibacterial activity was expressed as bacterial growth reduction in the presence of films with different Ferula oil concentration. Mean values with different letters within a column are significantly different by Duncan’s multiple range tests at p < 0.05. |  |  |  |  |